## Slide 1
ReAction Patch: Transdermal Steroid Drug Delivery Patch
Genna Felder, Miguel Hernandez, Hannah Radak, Anna Thomas, Daniel Fafemi
Faculty Advisor: Dr. Venkat K. Chivukula, Dept. of Biomedical Engineering, Florida Institute of Technology
Motivation
Results
Economics
Conclusions & Future Work
Acknowledgements
Design & Methods
Dr. Venkat Keshav Chivuluka, Nashaita Patrawalla, Dr. Christopher Bashur, Dr. James Brenner, MD/PhD Tatiana Karpova, Dr. Kishore, Karen at glassblowers.com, Aurora Burkus-Matesevac.
Develop a transdermal drug delivery patch system designed for topical steroid withdrawal tapering.
Determine the weight/volume of gelatin hydrogel most effective to deliver a therapeutic dose of steroid to a patient.
Test drug diffusion through Strat-M™, a skin-like membrane.
Figure 1. Comparison of layers of skin vs. layer composition of Strat-M™.
Determined the release profiles of different w/v gelatin hydrogels.
Perform cell studies on skin cells to get a better idea of the phenomenon of Topical Steroid Withdrawal.
Perform experiments with different materials and drug concentrations.
Fixed Costs | $12,072.90
Manufacturing Costs per Unit (Variable Costs) | $364,000
Retail Price (Box of 7 patches) | $40
Expected Units Sold | 64,000,000
Figure 2. Schematic representation of study. Gelatin-hydrocortisone hydrogels of 5% and 10% w/v were fabricated and crosslinked using glutaraldehyde. Hydrocortisone was diffused through Strat-M™ into the Franz cell in a 37°C incubator. Solution acquired from Franz cell was reacted with Tetrazolium Blue dye. The reacted product was then analyzed through a spectrometer and compared against a standard curve.
Objectives
Eczema affects nearly 31 million Americans.
Current treatment modality: suppression of symptoms with topical steroids.
Discontinuing the use of topical steroids can cause the patient to go through severe drug withdrawal.
ReAction patch aims to be a cost-effective solution to help patients experiencing drug withdrawal symptoms.
Figure 3. Comparison of 5%w/v and 10%w/v gelatin hydrogel diffusion over a 24 hour period. 5%w/v shows a controlled release profile. 10% w/v shows a burst release profile.
Figure 4. Statistical comparisons of several time points(TP) A) 4hr TP demonstrates that 10%w/v gelatin hydrogel has a burst release profile B) 8hr TP 5% w/v gelatin hydrogel has a higher release rate than 10%w/v C and D) 12hr and 24hr TPs confirm the results shown in B.